## Slide 1
Chaewon Jeon, and Kyoungsik Yu*
School of Electrical Engineering, Korea Advanced Institute of Science and Technology (KAIST), Daejeon 34141, Korea
*E-mail: ksyu@kaist.edu
Design of Polysilicon Grating Couplers using Metal Reflector in FD-SOI Platform
Introduction
Silicon photonics and zero-change integration
(a)
(b)
Silicon photonics exploits silicon as an optical platform to generate, modulate, and detect light, enabling high-bandwidth and energy-efficient data transmission
Zero-change integration leverages this CMOS compatibility to monolithically integrate photonic and electronic circuits on a single chip without modifying standard CMOS flows
FD-SOI Platform
(a)
(b)
A sub-10 nm device layer and a sub-100 nm buried oxide (BOX) layer are not suitable for efficient waveguiding and light coupling
Silicon substrate removal and additional SiO₂ deposition are required to form a symmetric refractive index profile around the waveguide
Grating coupler design
Theoretical backgrounds
Simulation result
Post-processing and measurement
Conclusion
The grating coupler couples light between an optical fiber and on-chip waveguides using a periodic structure
Back-reflection is suppressed by detuning the grating and tilting the fiber at a small angle (𝜃c), with a metal reflector added
Split grating couplers are used to distribute the coupled light into two waveguides under layout constraints
(a)
(b)
(a)
(b)
Type Ⅰ
Type Ⅱ
The spacing between parallel grating couplers reduces the coupling efficiency and shifts the peak wavelength to 1560 nm
Introducing a metal reflector improves the coupling efficiency to
−1.28 dB/facet
Post-processing
(a)
(b)
The silicon substrate was removed using a strong alkaline solution,
with the BOX acting as an etch-stop layer
A 1 μm SiO₂ layer was deposited on the BOX to form a symmetric cladding
Measurement result
(a)
(b)
The measured coupling efficiency of the grating coupler is approximately −32 dB/facet, mainly attributed to silicide-induced optical loss
To address this issue, a silicide blocking layer (SBLK) is introduced to prevent silicide formation
This study presents a grating coupler design methodology on the FD-SOI platform that avoids design rule violations.
The coupling efficiency was predicted to be −1.28 dB per facet in simulation, while the measured value was −32 dB per facet, attributed to silicide-induced optical loss in the polysilicon waveguide. A silicide blocking layer was introduced to mitigate this loss.
* The chip fabrication and EDA tool were supported by the IC Design Education Center(IDEC), Korea.